Second LACCEI International Latin American and Caribbean Conference for Engineering and Technology (LACCEI’2004)

“Challenges and Opportunities for Engineering Education, Research and Development”

2-4 June 2004, Miami, Florida, USA

Surface Modification of Carbon Nanotubes Using Poly (Vinyl Alcohol) For Sensor Applications

Harindra Vedala, M.S

Graduate Student, Florida International University, Miami, Florida, USA

Young Chul Choi, PhD

Research Scholar, Florida International University, Miami, Florida, USA

Gene Kim, PhD

Senior Staff Engineer, Motorola, Fort Lauderdale, Florida, USA

Eungmin Lee, M.S

Graduate Student, Florida International University, Miami, Florida, USA

Won Bong Choi, PhD

Associate Professor, Florida International University, Miami, Florida, USA

Abstract

Surface modification of the carbon nanotubes plays an important role for their utilization in various applications. In this study, single-wall and multiwall nanotubes were grown on a 1 cm2 silicon dioxide substrate using chemical vapor deposition. The surface of grown nanotubes was modified by polyvinyl alcohol and the wettability on nanotubes was investigated. This functionalisation tends to change the surface of nanotubes into hydrophilic thus increasing its sensitivity. The electrical characterization of these modified nanotubes was performed since it is expected that by adapting analytes onto the polyvinyl alcohol modified nanotubes, the electric transport property of CNT may be changed. Sensor applications of these modified nanotubes are also suggested.

Keywords

Carbon Nanotubes, Surface Modification, PVOH, Sensors, Nanosensors

1. Introduction

The excellent mechanical and electrical properties of carbon nanotubes make them attractive to various device applications including sensor applications. Single wall nanotubes have been synthesized into different shapes for various electronic applications (Choi and Choi, 2004).Single wall nanotubes have also been grown selectively to make nanoscale transistors (Choi et al., 2003). Carbon nanotubes based sensors have been shown to have detection capability for gas molecules such as NO2 and other organic vapors (Li et al., 2003). This sensing mechanism is attributed to the changes in the electrical conductivity of these nanotubes caused by the charge transfer from the gas molecule. Moreover due to their large surface area, carbon nanotubes have high sensitivity for gas and chemical vapors at room temperature as compared to conventional metal oxides sensors which operate at high temperatures. The gas sensing capability of the intrinsic nanotubes can be greatly enhanced by functionalisation with different molecules and functional groups.  Polymer coated carbon nanotubes have shown high sensitivity and selectivity for gases like NH3 and NO2 (Qi, et al., 2003). While other studies have shown that nanotube based polymer composites can be used for   strain sensing (Dharap, et al., 2004). Since carbon nanotubes are hydrophobic in nature they cannot be directly used for applications like relative humidity sensing. Polyvinyl alcohol (PVOH) is well known for its hydrophilic properties. It is atactic yet semicrystalline in nature which becomes surface-active at hydrophobic surface/water interfaces and concentrates at these sites allowing crystallization to occur. It is a water soluble polymer which is used in various industries such as textiles, adhesives, ceramics and paper. Recently its application as a polymer coating on a SAW device for improving the chemical sensing capability was shown (Kozlov et al., 2003), (Penza, et al., 1999). Earlier studies in which PVOH was used for functionalisation of carbon nanotubes mainly focused on improving the mechanical properties of nanotubes (Zhang et al., 2003). Here we present initial results of the effect of functionalisation by PVOH. The wettability behavior of nanotubes is studied as it plays a crucial role in adsorption and sensing of the analytes. These PVOH functionalised nanotubes may be used for sensing gases like CO and biomolecules which are not detected by pristine nanotubes.

2. Experimental Details

Carbon nanotubes were grown on 1cm2 SiO2/Si substrates using CVD process. Single wall tubes were grown on iron thin film at 900°C by using methane and ethylene as precursors, while multiwall carbon nanotubes were grown on the similar substrate at 700°C by using ethylene as precursor. The catalyst for all the samples were deposited by using spin coating method with speeds ranging from 500-1000 rpm. The functionalisation of the nanotubes was down by submersion of the substrate into aqueous solution of PVOH (99% hydrolyzed, MW-89-98K, obtained from Alfa Aesar), which was prepared by mixing PVOH with deionized water at the ratio 1:10000 (w/v) and heating at 90°C for 1 hour with constant stirring. The substrate was kept in the solution overnight, since the functionalisation of PVOH occurs while cooling. The substrates were then removed by rinsing with copious amount of deionized water and drying under vacuum.

To study the effect on the wettability of the carbon nanotubes by PVOH functionalisation, dynamic contact angles were measured by using contact angle analyzer. The contact angles of the functionalized CNTs were compared with that of the pristine carbon nanotubes. The electrical characterization was carried out by using probe station (Desert Cryogenics) coupled with semiconductor parameter analyzer (Agilent, 8146C). The IV characterization was conducted in vacuum conditions.

3. Results and Discussion

Figure 1 illustrates the SEM micrographs of multiwall carbon nanotubes before and after functionalisation with PVOH. It can be clearly seen that even a small amount (0.001 % w/v) of PVOH can significantly change the surface morphology of the nanotubes. In Figure 2 the effect on the water droplet deposited on the multiwall nanotubes before and after functionalisation is shown. The dynamic contact angles (advancing and receding) were measured for both single wall and multiwall carbon nanotubes. In Table 1 it can be seen that there is change in contact angle from 148 to 24 (advancing angle) corresponding to an average of 84% decrease when carbon nanotubes are functionalized. This clearly suggests that PVOH can be used for modifying the hydrophobic behavior of nanotubes to highly hydrophilic. The basic mechanism of interaction between the PVOH and nanotubes can be attributed to the lowering of interfacial free energy which is evident from the change in the contact angles of the functionalized nanotubes. PVOH tends to crystallize and introduce an alcohol functional group on the surface of the nanotubes. These functional groups can further act as intermediate for linking with various molecules which are to be sensed.

Figure 1: Multiwall carbon nanotubes without functionalisation (Left) and with PVOH functionalisation (Right)

Figure 2:  Effect on the water droplet deposited on the multiwall carbon nanotubes before (left) and after (right). (Size of each sample: 1 cm2)

Table 1: Effect of PVOH functionalisation on single wall and multiwall carbon nanotubes

|  | Advancing Angle | Receding Angle |
| --- | --- | --- |
| SWNT (Before Functionalisation) | 139.8 | 121 |
| SWNT (After Functionalisation) | 25.6 | 18.2 |
| MWNT 1 (Before Functionalisation) | 147.8 | 133.8 |
| MWNT 1 (After Functionalisation) | 23.6 | 19 |
| MWNT 2 (Before Functionalisation) | 148.2 | 139.8 |
| MWNT 2 (After Functionalisation) | 34 | 25.2 |
| SWNT: Single Wall NanoTube |  |  |
| MWNT: Multi Wall NanoTube |  |  |
| 0.001% w/v of PVOH in distilled water |  |  |

4. Conclusion

In this study single wall and multiwall carbon nanotubes were functionalized by using PVOH. It was shown that PVOH is able to modify the surface behavior of single or multiwall carbon nanotube from hydrophobic to highly hydrophilic. These findings are being further studied for possible use of functionalized carbon nanotubes for humidity, gas and bimolecular sensing. The IV characterization is also being studied to understand the charge transport mechanism in these modified carbon nanotubes.

5. References

Choi, Y.C., Choi, W., (2004) “Growth of Y junction single wall carbon nanotubes”, submitted to Advanced Materials.

Choi, W.B., Cheong, B.H., Kim, J.J., Ju, J., Bae, E., Chung, G., (2003), “Selective growth of carbon nanotube for nano-scale transistor”, Advanced Functional Materials, Vol. 13, pp 80.

Li, J., Lu, Y., Ye, Q., Cinke, M., Han, J. and Meyyappan, M., (2003). “ Carbon nanotube sensors for gas and organic vapor detection”, NanoLetters , Vol. 3, 7, pp 929-933

Qi, P., Vermesh, O., Grecu, M., Javey, A., Wang, Q. and Dai, H., (2000). “Towards large arrays of multiplexed functionalized carbon nanotube sensors for highly selective and sensitive molecular detection” NanoLetters, Vol. 3, No. 3, pp 347-351

Dharap, P., Li, Z., Nagarajaiah, S. and Barrera, E. V., (2004). “Nanotube film based on single wall carbon nanotubes for strain sensing”, Nanotechnology, Vol. 15, pp 379-382

Kozlov, M., Moon, S.I., Smith, T.A., McCarthy, (2003), “Adsorption and chemistry of ultra –thin films of polyvinyl alcohol for sensor development”. Polymer, Vol. 44, No.2, pp 283.

Penza, M., Anisimkin, V.I., (1999), “Surface acoustic wave humidity sensor using polyvinyl alcohol film”, Sensors and Actuator, Vol. 76, pp 162-166

# Text boxes

## Figure 1. Dimensions of final proceedings page

Times New Roman Font, Size 8 pt, Italic, Single spacing, Left Justify

(This text must be typed by the authors and should appear on the first page only)

First Level Heading

Times New Roman Font, Size 12 pt, Title Case, Bold

Abstract Section Title

Times New Roman Font, Size 12 pt, Title Case, Bold

Times New Roman Font, Size 11 pt, Bold, Single spacing, Center

Figures must centralized

Times New Roman Font, Size 11 pt, Single spacing, Center

Paper Title

Times New Roman Font, Size 14 pt, Title Case, Bold, Single spaced, Center

Keyword Section Title

Times New Roman Font, Size 12 pt, Title Case, Bold

Author

Times New Roman Font, Size 11 pt, Bold, Single spacing, Center

Conference Identification  Heading

Times New Roman Font, Size 9 pt, Italic, Single spacing, Left Justify (This text must be typed by the authors and should appear on the first page only)

Times New Roman Font, Size 10 pt, Bold, Single , spacing, Center

Author Affiliation

Times New Roman Font, Size 11 pt, Single spacing, Center

Figures must be placed in the center of the page

21 cm

29.7 cm

3 cm top margin

Side and bottom margins

2.5 cm each

Second Level Heading

Times New Roman Font, Size 11 pt, Title Case, Bold

Third Level Heading

Times New Roman Font, Size 11 pt, First Letter Capital, Bold